## Slide 1
ETCH TB Library Summary
----Arcing

## Slide 2: TB Library Summary
TB Library 主要从以下几方面阐述：
  失效机理
  鱼骨图
  具体案例
  解决方案

## Slide 3: Arcing 失效机理
Arcing 主要由以下一种或几种失效机理产生:
  后段特殊的MIM结构: Backend structure especially with MIM layer is easy to collect electron and electron current will induce arcing.
  Wafer edge exposed metal with abnormal horizontal E-field
  Wafer edge exposed metal overhang esc as sparkle for arcing
  Current starts to flow when resistance reach critical low value
  Current starts from edge through metal, via and substrate
  Arcing current tried to find the shortest path back to plasma
  “Snake defect” is the burned metal residue from arcing current passing
  Chamber polymer peeling into plasma, polymer表面吸附大量电荷局部电压过大引发arcing.
  Chamber RF system not stable, plasma unstable induce arcing.

## Slide 4: Arcing 鱼骨图
Machine
Method
Etch recipe
(power magnet transition)
Material
Tool type difference
N2 Purge
Arcing
Environment
WET clean/ Scrubber
Humidity
Gas purity
Chemical Conc.
Chamber peeling
Baking
(Before or post)
Q-time
Parts damage
Asher Temp.
Incoming wafer: charging
Temp
Wafer edge metal exposure
Process by product metal element
1
2
5
6
7
9
8
3
10
11
4
15
14
13
12
16

## Slide 5: Arcing 解决方案
从其失效机理来分析，Arcing 的解决方案主要为:
  MIM structure is easy to collect electron and electron current will induce arcing.
  Reduce VIA etch OE step RF power, magnet intensity.
  Chamber polymer peeling into plasma, polymer表面吸附大量电荷局部电压过大引发arcing.
  Control cathode/wall liner roughness, reduce polymer peeling probability
  Chamber RF system not stable, plasma unstable induce arcing.
  Check chamber RF system include RF generator, RF match, RF cable, magnet driver etc
  Tighten RF related IEMS parameter (RF forward mean, dev, RF reflect mean dev etc）
  Recipe optimization to keep stable plasma environment

## Slide 6
Thank You

## Slide 7
Case 1: B1 EEOXA11_AC Wafer Arcing
7
Issue Description:
90Nor suffered 3pcs wafer arcing in producer chamber(EEOXA11_A 2pcs (E5B946#02 4464; E5E060#03 4395) EEOXA11_C 1pcs (E5B998#04 4464).
Root Cause:
  WEE AL exposure caused by 90Nor wafer edge baseline compile with EPILS01 condition worse.
  Solution: WEE optimization. PIE 2/15

## Slide 8
Case 2: B1 Wafer Edge W Induced Arcing
Issue Description:
From 9-24 to now, total 5pcs (E5Q929 #22/ E5P997 #13#19#23 /E5Q912 #2 ) suffered arcing issue and defect high at V1OX-ET
Root cause: Suspect W remain at wafer edge, lead to micro-arcing after main etch
Solution:
TF check ETWDP02_B. TF

## Slide 9: Case 3: F8 Vx ET wafer edge W arcing
Issue Description:
  Vx ET suffer wafer edge W arcing defect.
  IEMS&DA can not getting.
Root Cause:
  W DEP condition NG, dedicate to W EDP worse chamber.
Action:
  Constrain W DEP worse chamber.
Ball defect
EDX 10000V
W peak

## Slide 10: Case 4: S1 D13 2037 Via Arcing
Issue description:
  2037 15pcs wafer from 14 lots suffered SWLY with same pattern from 2008/11/25, by wafer yield loss 75%~100%,
  Arcing take place during V7OX_ET, arcing source all from PHOTO zero mark area
Root cause:
  Arcing happen during V7 etch through TaN/Ta film and wide M5 at the boundary between M5 & MIM PHOTO REMA shielded area.
Solution:
Change MIM_PHOTO process to expose the area around zero mark
Arcing source!!!
M5 Cu
TaN/Ta
Partial die
TaN/Ta film

## Slide 11: Case 5: F7 TEL TV-ET suffer arcing defect
Issue Description:
  18MS TV-ET suffer arcing defect if there is MIM layer under TV
Root Cause:
  There is permanent magnet on TEL DRM, so the plasma density is stronger than eMax(magnet can be turned off), which lead to wafer arcing.
Solution:
  Constraint all TV-ET on TEL for all flow which had MIM structure

## Slide 12: Case 6: F7 EMAX polymer peeling arcing
Issue Description:
  18MS TV-ET suffer arcing defect if there is MIM layer under TV
Root Cause:
  Chamber polymer peeling into plasma, polymer表面吸附大量电荷局部电压过大引发arcing.
Solution:
  Control cathode/wall liner roughness, reduce polymer peeling probability

## Slide 13: Case 7: F7 Super-e AR ET arcing
Issue Description:
  AR ET suffer arcing defect .
  Some impact wafer RR13_MAX and RR13_DEV jump
Root Cause:
  Chamber RF system not stable, plasma unstable induce arcing.
Solution:
  Change RF generator
  Tighten RR13_MAX and RR13_DEV limit.

## Slide 14
Case 8: F8 Vx ET wafer edge arcing
Issue Description:
  Vx ET suffer wafer edge CU arcing and SI/O arcing. (residue type or surface type)
  IEMS&DA can not getting.
Resiude 1
Resiude 2
Surface PD
CU peak
Root Cause:
  Not clear, suspect wafer edge condition NG
Containment Actions:
  Tighten chamber RF time
  Survey install 2 stage pin follow WW